Development of Mathematical Model and Identification of Optimal Conditions to Obtain Phenol-Cresol-Formaldehyde Resin

Yuriy Demchuk1, Serhiy Pyshyev1, Mariia Shved 1, Volodymyr Gunka1, Solomiya Bratash2, Roman Pyryk3

1. Department of Chemical Technology of Oil and Gas Processing, Lviv Politechnic National University, UKRAINE, Lviv, S. Bandery street 12, E-mail: yuriy_demchuk@ukr.net
2. Department of Automated Control Systems, Lviv Politechnic National University, UKRAINE, Lviv, S. Bandery street 12, E-mail: solomijka99@gmail.com
3. Department of Highways and Bridges, Lviv Politechnic National University, UKRAINE, Lviv, S. Bandery street 12, E-mail: romapyryk@gamil.com

Abstract ( The effect of factors on the process of obtaining phenol-cresol-formaldehyde resin (PhCR-F) has been studied. By using empirical evidence, the adequate experimental statistical-mathematical (ESM) model has been developed. Based on this model, the optimal values of the process factors for obtaining PhCR-F have been identified, bringing about both high yield and softening point of the resin. Data predicted on the basis of the ESM model were compared with empirical evidence about PhCR-F preparation.lace here short abstract of the proceedings.

Кеуwords ( phenol-cresol-formaldehyde resin, optimal conditions, experimental statistical-mathematical (ESM) model, modifier, bitumen.

Introduction

At present, in terms of fast traffic volumes common asphaltic concrete based on unmodified bitumen is not able to provide desired physical and mechanical properties as well as durability of road surfaces. One of the directions in enhancing the quality of bitumen for making road pavements with good performance characteristics is to improve the structure and properties of bitumens by modifying them with polymeric materials.

For copolymers owing to their capability not only to increase the bitumen strength, but also impart elasticity to a polymer bituminous mixture modification of road bitumens, thermoplasts are most commonly used (mainly, SBS-type styrenic block-, specifically at lower temperatures, and also increase adhesion of bitumen with a mineral material. The content of such polymers in modified bitumens may account for 3–10 wt % [1-5].

The main disadvantage restricting the growth rate of producing thermoplastic elastomer-modified bitumen is their high cost (1.5–2.5 times greater than the cost of unmodified bitumen) [1, 2]. It is, therefore, important to search for inexpensive substances that improve the performance of bitumens and, primarily, their adhesive properties.

At the Department of Chemical Technology of Oil and Gas Processing, Lviv Polytechnic National University, the possibility of using modified phenol-formaldehyde resin (PFR) as additives to petroleum bitumen was trailed. These studies show that the said resin has proved to improve a range of performance characteristics of bitumens, most notably, the adhesion.

Consequently, the idea was put forward to investigate the use of PFR derived from relatively cheap raw materials. The phenolic fraction was used as a feedstock collected from coke and chemical plants in Ukraine. Additionally, feedstock contains other than phenols relatively large amounts of cresols; therefore, accordingly, phenol-cresol-formaldehyde resins (PhCR-F) were yielded. In publications reported by authors [6-7], the manner PhCR-F is obtained from a phenolic fraction and the application of PhCR-F as modifiers of bitumen was investigated.

While using this modifier, a significant enhancement is observed in the adhesive properties of the domestic petroleum bitumens, enabling a strong relationship between a film of bitumen and a surface of mineral materials. This allows the life of the road surface to be extended and significantly improve its durability.

To define optimal conditions of the mechanism of PhCR-F preparation, a series of experiments was carried out. The development of experimental statistical-mathematical (ESM) model was justified by this empirical evidence. This model covers dependencies of main response functions on the process factors, and on its basis the optimal conditions of obtaining PhCR-F can be predicted.

Experimental

The phenolic fraction of coal tar was withdrawn at JSC “Zaporizhkoks” (Ukraine).

To obtain the modified bitumen, we used the oxidized bitumen BND 60/90 produced by PJSC “Transnational financial and industrial oil company Ukrtatnafta” (Kremenchuk, Ukraine).

Novolac phenol-cresol-formaldehyde resin was obtained according to the scheme given in Fig.1 by the method of formaldehyde condensation polymerization with the “raw” phenols extracted from these fractions.

Fig.1. Scheme of researches: WPhF ( wide phenolic fraction; RPh – “raw” (technical) phenols; PhCR-F – phenol-cresol-formaldehyde resin.

Results

It was necessary to develop the ESM model of the process of PhCR-F preparation, verify the adequacy of the former, and find the optimal process conditions. By analyzing experimental data, the intervals that change the main factors of the process have been selected for the ESM model development, such as the catalyst concentration of 0–6 wt %; the mass ratio of the components 1.78–3.80; the temperature 318–373 K; the duration 5–120 min.

In describing the process of obtaining PhCR-F using the ESM model, the following designations were used for the response functions and main control factors of the process: Y1 is the resin yield, wt %; Y2 is the ring-and-ball softening point, (ºС); X1 is the concentration of a catalyst, wt %; X2 is the mass ratio of components; X3 is temperature, ºС; X4 is the process duration, min.

For the response functions, various types of dependencies on the process factors were developed and, finally, resulting in the choice of non-linear models as they showed the best fit to the experimental data. For defining the equations of multiple regressions (1) and (2), the STATISTICA software package was used

| Y1= –41.7817 – 1.19464∙Х12 – 8.63368∙Х22 + 0.001537·Х32 – 0.001700∙Х42 – 211.626∙Х1∙Х2 – 1.90101∙Х1∙Х3 + 11.65319∙Х1∙Х4 + 4.327906∙Х2∙Х3 + 5.019971∙Х2∙Х4 – 0.293050∙Х3∙Х4 – 121.787∙Х1 – 72.6620∙Х2 + 15.872311∙Х3 – 14.2770∙Х4 | (1) |
| --- | --- |
| Y2= –30.3736 – 2.19792∙Х12 – 3.70991∙Х22 + 0.007490·Х32 – 0.005547∙Х42 – 154.004∙Х1∙Х2 – 1.40209∙Х1∙Х3 + 8.707432∙Х1∙Х4 + 2.707432∙Х2∙Х3 + 3.537820∙Х2∙Х4 – – 0.2113198∙Х3∙Х4 – 88.5967∙Х1–52.8532∙Х2 + 11.80819∙Х3 – 10.0859∙Х4 | (2) |

By substituting the values of X1-X4 in all the above equations, the expected values of the response functions (Yijreg) and relative ESM errors (ε1 for Y1; ε2 for Y2) were found for each experiment. Table 1 lists all these values. The models’ adequacy was checked using regression response functions.

Table 1

# Experimental data, calculated values of response functions and relative errors

| Entry | X1, wt% | X2 | X3, °С | X4, min | Y1, wt% | Y1reg, wt% | Y2, °С | Y2reg, °С | Relative errors |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  | ε1 | ε2 |
| 1 | 0 | 1.78 | 100 | 60 | 69.3 | 72.89 | 58 | 75.00 | 0.0518 | 0.2931 |
| 2 | 1 | 1.78 | 100 | 60 | 88.5 | 82.30 | 119 | 92.31 | 0.0700 | 0.2243 |
| 3 | 2 | 1.78 | 100 | 60 | 90 | 89.33 | 115 | 105.23 | 0.0074 | 0.0849 |
| 4 | 3 | 1.78 | 100 | 60 | 94.3 | 93.96 | 110 | 113.75 | 0.0035 | 0.0341 |
| 5 | 6 | 1.78 | 100 | 60 | 94.3 | 93.53 | 117 | 112.95 | 0.0081 | 0.0346 |
| 6 | 3 | 1.78 | 100 | 60 | 94.3 | 93.96 | 110 | 113.75 | 0.0035 | 0.0341 |
| 7 | 3 | 2.2 | 100 | 60 | 88.5 | 90.22 | 95 | 94.18 | 0.0195 | 0.0086 |
| 8 | 3 | 2.72 | 100 | 60 | 81.9 | 81.36 | 82 | 68.14 | 0.0065 | 0.1691 |
| 9 | 3 | 2.86 | 100 | 60 | 79.4 | 78.18 | 60 | 60.78 | 0.0153 | 0.0131 |
| 10 | 3 | 3.05 | 100 | 60 | 73.3 | 73.32 | 47 | 50.57 | 0.0003 | 0.0759 |
| 11 | 3 | 3.3 | 100 | 60 | 65.2 | 65.98 | 23 | 36.72 | 0.0120 | 0.5966 |
| 12 | 3 | 3.8 | 100 | 60 | 48.12 | 48.05 | 14 | 7.63 | 0.0013 | 0.4547 |
| 13 | 3 | 1.78 | 45 | 60 | 75.5 | 74.94 | 74 | 74.39 | 0.0074 | 0.0053 |
| 14 | 3 | 1.78 | 60 | 60 | 78 | 79.21 | 82 | 80.63 | 0.0155 | 0.0166 |
| 15 | 3 | 1.78 | 80 | 60 | 86.4 | 85.97 | 91 | 94.20 | 0.0050 | 0.0352 |
| 16 | 3 | 1.78 | 90 | 60 | 90.4 | 89.81 | 106 | 103.23 | 0.0065 | 0.0262 |
| 17 | 3 | 1.78 | 95 | 60 | 92.5 | 91.85 | 109 | 108.30 | 0.0070 | 0.0064 |
| 18 | 3 | 1.78 | 100 | 60 | 94.3 | 93.96 | 110 | 113.75 | 0.0035 | 0.0341 |
| 19 | 3 | 1.78 | 100 | 5 | 82.5 | 82.82 | 79 | 77.82 | 0.0039 | 0.0150 |
| 20 | 3 | 1.78 | 100 | 10 | 86.5 | 84.26 | 84 | 82.47 | 0.0259 | 0.0182 |
| 21 | 3 | 1.78 | 100 | 20 | 85.8 | 86.88 | 89 | 90.95 | 0.0126 | 0.0219 |
| 22 | 3 | 1.78 | 100 | 40 | 86.3 | 91.10 | 96 | 104.57 | 0.0557 | 0.0893 |
| 23 | 3 | 1.78 | 100 | 60 | 94.3 | 93.96 | 110 | 113.75 | 0.0035 | 0.0341 |
| 24 | 3 | 1.78 | 100 | 90 | 93.8 | 95.71 | 113 | 119.21 | 0.0204 | 0.0550 |
| 25 | 3 | 1.78 | 100 | 120 | 94.6 | 94.39 | 116 | 114.68 | 0.0022 | 0.0113 |
| Average relative errors of approximation (ε) | 0.0147 | 0.0957 |

While making an evaluation of the adequacy of equations (1) and (2) the patterns below were established.

The major portion of residuals ∆Yij=Yіjreg– Yіjas shown in histograms and plots of probit (Fig. 1-4) is centered around zero, signifying the first mandatory characteristic of the normality of resulting equations.

| ΔY1 | ΔY2 |
| --- | --- |
| Fig. 1. Histogram of ΔY1 residuals | Fig. 2. Histogram of ΔY2 residuals |

| ΔY1 | ΔY2 |
| --- | --- |
| Fig. 3. Plot of probit for ΔY1 residuals | Fig. 4. Plot of probit for ΔY2 residuals |

The average relative errors of approximation are as follows: ε1 = 0.0147 (1.47%), ε2 = 0.9566 (9.56%). As reported in [11] at ε equal to 0–10 % the precision of prediction is high, at ε = 10–20 % – good, and at ε = 20–50 % –satisfactory. From this it can be claimed that the built models have a high agreement with experimental evidence.

The estimated values of the Fisher criterion are F1 = 22.53 and F2 =7.54. According to the table of Fisher criterion values [12],at the level of significance α of 0.05 the critical values are defined as F1cr= F2cr = F(0.05; 24; 10) = 2.74.That is, they are less than that calculated which also proves the normality of the model.

The coefficients of determination are R12 = 0.9693 and R22 = 0.9135. In other words, 96.93% and 91.35% of changing a response function (Y1 and Y2, respectively) are determined using the preferred control factors of the process (Х1 – Х4).

The estimated values of the statistical criterion are F1r= 22.53 and F2r= 7.54. As shown in the table of Fisher criteria, the critical values are given as F1rcr = F2rcr = F(0.05; 14; 10) = 2.86 at the level of significance α of 0.05. This clearly demonstrates the statistical significance of coefficients of determination Rі2 (Fircr<Fir).

These figures signify the adequacy of the ESM process in which PhCR-F was prepared, the statistical significance of results and the presence of a strong relationship between response functions and preferred control factors of the process.

On the basis of the regression equations, the optimal process conditions were found by the method of uniform search for the values of the response functions and that would ensure the maximum yield of PhCR-F and softening point of the resulting resin.

The calculated optimal values of the process parameters (X1 = 1.85 wt%; X2 = 2.15; X3= 104.5 ºС; X4= 69 min) and estimated (predicted, Yіreg) values of response functions are listed in Table 2.

Table 2

Optimal conditions of PhCR-F synthesis

| Process parameters | Response function value |
| --- | --- |
| X1, wt% | X2 | X3,°С | X4, min | Y1, wt% | Y1reg, wt% | Y2, °С | Y2reg,°С |
| Calculated values |
| 1.85 | 2.15 | 104.5 | 69 | - | 95.0 | - | 85 |
| Experimental values |
| 2.06 | 2.16 | 105.0 | 69 | 92.5 | - | 92 | - |

The synthesis of PhCR-F carried out under conditions as close as possible to optimal (X1 = 2.06 wt%; X2 = 2.16; X3 = 105 ºС; X4 = 69 min) resulted in a sufficiently high yield of the major product (the resin) – 92.5 wt% and its high softening point – 92 °С. The relative difference between the experimental and predicted values amounts to 2.70% (for Y1) and 7.61% (for Y2).

The resulting resin was used as an adhesive additive to modify oxidized road bitumem. In accordance with industrial requirements the amount of modifier approx. 1 wt % is technically and economically feasible; so we studied bitumen modification adding 1 wt % of PhCR-F. Characteristics of the obtained PMB are given in Table 3.

Table 3

Physico-mechanical parameters of pure and modified bitumen

| Bitumen | Parameters |
| --- | --- |
|  | Softening point R&B, K | Penetration at 298 K, 0.1 mm | Ductility at 298 K, m·10-2 | Fraass breaking point, K | Plasticity range, K | Penetration index | Adhesion to |
|  |  |  |  |  |  |  | crushed stone, points | glass, % |
| BND 60/90 | 319 | 70 | 63 | 255 | 337 | -1.5 | 3 | 33 |
| BND 60/90 + PhСR-F (1.0 wt %) | 321 | 68 | 46 | 255 | 339 | -0.9 | 5 | 87 |

One can see from the obtained results that addition of PhCR-F in the amount of 1 wt % to bitumen changes the following characteristic:

- the softening temperature is increased by 2 К;

- elasticity (penetration and ductility) is slightly degraded, though plasticity interval is increased;

- adhesive properties are considerably improved (from 33 to 87 %).

Conclusion

A quadratic experimental statistical model of the process to prepare the phenol-cresol-formaldehyde resin from the phenolic fraction of the coal tar has been developed. The adequacy and statistical significance of the model has been proved on the basis of four parameters.

The optimal process conditions were found (X1 = 1.85 wt%; X2 = 2.15; X3 = 104.5 ºС; X4 = 69 min), and 92 °С softening point of the resin was produced. The resin yield was 92.5 wt% for a starting material.

Applying the developed ESM model we can fairly accurately predict the amount of the resulting resin and its main characteristic (a softening point by the ring-and-ball method). The resin prepared under predicted conditions based on the ESM model was proved to have a greater yield and a higher softening point than those found in the previous studies. This PhCR-F will be used further for modification of road bitumens and derived bituminous emulsions.

References

[1]	Zhu, J. (2014). Polymer modification of bitumen: Advance and challenges irgisson. European Polymer Journal, 54, 18-38.

[2]	Pyshyev, S. V. (2016). Polymer modified bitumen: Rewiew. Chemistry & Chemical Technology, 10, 63-636.

[3]	Kowalski, K. J. (2016). Eco-friendly materials for a new concept of asphalt pavement. Transportation Research Procedia, 14, 3582-3591.

[4]	Schaur, A. (2017). Impact of molecular structure of SBS on thermomechanical properties of polymer modified bitumen. European Polymer Journal, 96, 256–265.

[5]	Kishchynskyi, S (2018). Physical and chemical properties of bitumen, modified, modified by the complex modifier Polyd. Vestnyk Kharkovskogo natsinalnogo avtomobil`no-dorozhnogo universytetu, 40, 28-32.

[6]	Demchuk, Y. Y. (2017). Oderzhannia modyfikatoriv dorozhnikh bitumiv z fenolnoi fraktsii kamianovuhilnoi smoly [Obtaining of the modifiers of road bitumen from phenol fraction of coal tar]. Uglekhimicheskii zhurnal, 5, 23-28.

[7]	Demchuk, Y. Y. (2018). Effect of phenol-cresol-formaldehyde resin on adhesive and physico-mechanical properties of road bitumen. Chemistry & Chemical Technology, 12, 456-461.

[8]	Toroptseva, A. (1972). Laboratornyi praktikum po khimii i tekhnologii vysokomolekuliarnykh soedineniy [Laboratory practicum on chemistry and technology of high-molecular compounds]. Moskva: Khimiya.

# Text boxes

WPhF

Removal of “raw” phenols

RPh

Polycondensation with formaldehyde

PhCR-F

Bitumen modification